## Slide 1
Prof. Dr. Kornelius Nielsch
Institute for Metallic Materials (IMW), IFW Dresden
Energiewandlung mittels Nanostrukturierte Thermoelektrika

## Slide 2
Licht
Elektrizität
Mechanik
Wärme
Brennstoff
Verbrennung
Wärmekraft-
maschinen
Generator
Photovoltaik
Photosynthese
Brennstoffzelle
Konventionelle Stromerzeugung: 90% der Stromgewinnung
MPI-MSP Halle
SPP 1386
Thermoelektrik

## Slide 3
Stromerzeugung aus Wärme im Auto
Viel Wärme aus dem Auspuff
Energierückgewinnung
durch Thermoelektrik
Thermoelektrischer
Generator im KFZ
Quelle: BMW AG
Quelle: IAV GmbH
Nur ~ 1/3 der Gesamtenergie steht dem KFZ zum direkten Antrieb zur Verfügung
SPP 1386

## Slide 4: Cassini-Sonde
Die Cassini-
Sonde bezieht ihre
Energie aus der
Zerfallswärme von
Plutonium, die
thermoelektrische
Konverter (Inset)
in Strom umwandeln.

## Slide 5
Thermoelectric Applications
SPP 1386

## Slide 6
Thermoelectric Efficiency: ZT
ZT = T ~ 0,5-1
S2 

High Output Potentials: Seebeck coefficient
Low Thermal Conductivity
High Electric Conductivity
Elect. Conductivity ()
Therm. Conductivity ()
Glass
Diamond
Metal
Thermoelectrics

## Slide 7
Historischer Hintergrund: Thermoelektrik
Thomas Johann Seebeck
Seebeck-Effekt
1820
1840
- Peltier-Effekt
- Seebeck-Effekt
- Ohm‘sche Gesetz
1940
- PbS-Generatoren
1960
- Kühlung mit Bi2Te3
1990
2000
- Theorie zu TE Nanostrukturen
- TE Nanostrukturen ZT = 2-3
Berlin 1821
SPP 1386

## Slide 8: Functionality of Thermoelectric Modules
Continuous current
Heat emission
Price: 2 to 15 U$
Ca. 90% of moduls based on Bi2Te3
Handcrafted manufacturing

## Slide 9: Important Thermoelectric Materials
Room Temperature
Temperature (K)

## Slide 11
Thermoelectric Materials of the 20th Century
year

## Slide 12: Design Challenges
ZT = ---------- T
S2 

 = e + PH

## Slide 13
Promising approaches to higher ZT

## Slide 14: Overview of Thermoeletric Materials
Notes: 14

## Slide 15: Seltene Elemente für die Thermoelektrik
Bi

## Slide 16
Thermoelectric Materials

## Slide 17
Predictions for Confined Structures
Does not include deleterious interface or barrier effects
ZT enhanced by degeneracy: multiple carrier pockets in k-space
Hamburg, Jan 2013

## Slide 18: Template-based Synthesized of TE Nanowires
M. S. Sander, A. L. Prieto, R. Gronsky, T. Sands, A. M. Stacy,
Adv. Mater. 14, 665 (2002).
W. Wang, X. Lu, T. Zhang, W. Jiang, X. Li,
J. Am. Chem. Soc. 129, 6702 (2007).
Large-Area Bi2Te3 Nanowire Arrays into Porous Anodic Alumina Templates
Bi2Te3/Te Multiple Heterostructure Nanowire Arrays by Confined Precipitation

## Slide 19: Single Electron Transistor: Thermopower Measurements of InAs Nanowire with embedded Quantum Dot
E.A. Hoffmann, H. Linke et al., Nano Lett. 9, 779 (2009)

## Slide 20
Power-Factor Measurements of Backgate-tuned InAs Nanowire
Vapor-Liquid-Solid Growth of InAs Nanowires
Seebeck Characterization Setup with InAs Nanowire
In collaboration:
H. Linke and K. Nielsch et al., Nano Letters 13, 4080 (2013).
Notes: Measurement of Seebeck Coefficient and elektrical Conductivitiy under the influence of electrical fields
MOSFET-Setup
Tuning the Fermi-Level by E-Field
Quantized conductivity,
Quantendot-like behaviour
Very high power-factor

## Slide 21
Thermoelectric Properties of an Individual Bi0.39Te0.61 Nanowire
D. Kojda, et al, Sem. Sci. Tech. (2014).
ZTNW1 = 0.08 and ZTNW2 = 0.07

## Slide 22
TE two channel-model for Bi2Te3 put to the test. Experimental survey for Bi2Te3 from micro- to nanostructures
S / V ratio
nanostructure
bulk
TI two channel-model represents experiments for Bi2Te3 very well.
Notes: How does the two channel model for Bi2Te3 compare to experiments?
So it seems the model works fine for how Bi2Te3 we also applied the model to Sb2Te3 and BI2Se3

## Slide 23
Electrical Transport of Sb2Te3-Nanowires under Magnetic Fields
R Surface
R Bulk
Bulk
Surface

## Slide 24
Electric field-dependent Shubnikov-de Haas spectra of a Bi2Te3 nanowire
Linear dispersion relation is observed by transport measurements
J. Gooth et al., APL. 104, 243115 (2014)
2D and 1D Transport in Cylindrical NWs under Transverse Magnetic fields
S. Baessler et al , APL. 107, 181602 (2015)
Oscillations cannot be explained
by 2D surface or 3D bulk states
Landau Levels

## Slide 25
Electric field-dependent Shubnikov-de Haas spectra of a Bi2Te3 nanowire
The linear dispersion relation is observed by transport measurements
J. Gooth et al., APL. 104, 243115 (2014)
2D and 1D Transport in Cylindrical NWs under Transverse Magnetic fields
S. Baessler et al , APL. 107, 181602 (2015)
Oscillations cannot be explained
by 2D surface or 3D bulk states
Landau Levels

## Slide 26: Thermionic Energy Converters: Principles
Solid State Thermionic Device
Vacuum based Thermionic Device
Metal
Metal
Semi-conductor
Metal
Metal
Vacuum
Basic Concept: W. Schlichter, Germany, 1915
Lab demonstration (cesium vapor diode):
M. Y. Gurtovoy and G. I. Kovalenko, USSR, 1941
Pioneers: G.D. Mahan and A. Shakouri, USA, 1994/1997
Notes: Erklärung Thermionic
Glühemission von Elektronen ins Vakuum
Versuchsapperaturen mit 10% Effizienz
Anwendung auf Satelliten
Einige Aktivität in jüngster Zeit mit MEMS-Strukturen
Neue Ideen Photonunterstützte Thermoemission
Gegenkonzept: Thermionic auf Basis von Festkörperen
Realisierung mit III-V-Halbleritern und Festkörpern
Große experimentelle Herausforderung beim Wachstum

## Slide 27: Thermal Conductivity of Epitaxial Ge/Si Nanodot Multilayers
G. Pernot et al., Nature Mater. 9, 491-495 (2010).
IIN (IFW)
A. Rastelli & O. G. Schmidt

## Slide 28
Si thin films [Si13]
VLS Si NWs [Si12]
EE Si NWs [Si11]
SNAP Si NWs [Si10]
Integrated Si NWs [Si9]
Comparison of Silicon Nanowires: Thermal Conductivity
A. Majumdar et al., Nano Lett. 10, 4341 (2010).
Top Down: Electrochemical Etched Silicon Nanowires

## Slide 29
Thermoelectric Nanostructures (ZT >1)
State of the Arte for Devices: ZT < 1
ZT~3.5 @ 575 K
quantum dot superlattice (MBE)
n-type, PbSeTe/PbTe
[Harman, MIT-LL, J. Elec.Mat. 2000]
ZT~2.4 @ 300 K
superlattice (CVD)
p-type, Bi2Te3/Sb2Te3,
[Venkatasubramanian, RTI/Nextreme, 2001]
ZT~2.2 @ 800 K
bulk – ‘natural’ nanodots
n-type, AgSbTe2-PbTe (‘LAST’)
[Kanatzidis, Northwestern, 2004]
ZT~1.2 @ 350 K Nanowire p-type, Si
[Heath, Caltech, 2008]
ZT~0.6 @ 300 K
nanowire
p-type, Si
[Yang/Majumdar, Berkeley, 2008]
ZT~1.4 @ 373 K
bulk – fine grain
p-type, (Bi,Sb)2Te3
[15 authors, BC/MIT/GMZ Energy/Nanjing
University, 2008]

## Slide 30
Synthesis of Nanograined Bulk-Materials

## Slide 31: Overview: Nanograined TE Bulk Materials
K. Nielsch et al., Adv. Energy Mater. 1, 713 (2011).

## Slide 32: Nanopowder synthesis from the gas phase
J. Phys. D: Appl. Phys. 48, 314010 (2015).
J. Phys. D: Appl. Phys. 44, 174034 (2011).
Atmospheric pressure;
High cooling rate
Reduced pressure;
High cooling rate
Atmospheric pressure;
Low cooling rate
Synthesis: Group of H. Wiggers, University of Duisburg-Essen

## Slide 33: Si + WSi2 nanocomposites
Si + 5 % W
1 µm
J. Phys. D: Appl. Phys. 48, 314010 (2015).
50 nm
TEM by Mathis Müller and Hans-Joachim Kleebe, TU Darmstadt

## Slide 34
www.spp1386thermoelectrics.de/
Berlin, Oct 2010

## Slide 35
German Priority Program SPP 1386 on Nanostructured Thermoelectrics
May 2007 Overview Publication in Physik Journal
Sep 2007 Planning Meeting in Fulda
Nov. 15 Submission for the Founding Proposal
Apr. 2008 Positive Announcement about SPP 1386
Jul 2008 Network Meeting in Hamburg (80 Part.)
Sep. 22 Submission of 35 Proposals
Dec 2008 Selection of the Projects
Apr. 2009 Start of the individual Projects (18)
2009 to 2012 First Funding Period
2012 to 2015 Second Funding Period

## Slide 36: Funding from the German Ministry of Education and Science (BMBF) via the Material Development Program (WING)
WING Projects
with Industry
Product-
development
Market
Entry
Idea
Basic
Research
Materials for Tomorrow:
Scientific Pre-Project
Funding Focus
(z.B. Thermopower)
  5 Research Consortia
  17 Research Center involved, 5,5 Mio. €
10 funded Projects (ca. 27 Mio. €)

## Slide 37
Motivation: Electrochemical Synthesis of TE Films and Nanostructures
Sb2Te3 ; (Bi1-xSbx)2Te3
Miniaturized TE Devices
Flexible TE Devices
Notes: Kostengünstig zu Sputter-Technik
Electrochemie kann wesentliche Verbindungen erzeugen
Wässerige Lösungen
Zwei Konzepte

## Slide 38: Thematische Schwerpunkte in ThermoPower
Materialentwicklung für Temperaturbereich von 200°C – 1000°C
  Ressourcenverfügbarkeit
  Industrielle Herstellbarkeit
  Wirtschaftlichkeit
  Umweltverträglichkeit (Bismut-, Bleitellurid)
Systementwicklung
  maßgeschneiderte Aufbau- und
  Verbindungstechnik
  komplettes thermoelektrisches System
  Demonstrator
Begleitende Maßnahme
  Standardisierung von thermoelektrischen Referenzproben
  Etablierung von validierten thermoelektrischen Meßmethoden
Quelle: IAV GmbH

## Slide 39: Funding from the German Ministry of Education and Science (BMBF) via the Material Development Program (WING)
WING Projects
with Industry
Product-
development
Market
Entry
Idea
Basic
Research
Materials for Tomorrow:
Scientific Pre-Project
Funding Focus
(z.B. Thermopower)
  5 Research Consortia
  17 Research Center involved, 5,5 Mio. €
10 funded Projects (ca. 27 Mio. €)

## Slide 41: The Great Vision for Thermoelectric: Waste Heat Recovery

## Slide 42: The Great Vision for Thermoelectric: Waste Heat Recovery

## Slide 43
Thermoelectric Society of Japan: Academic Roadmap for TE Applications
2040
2030
2020
2010
10-6
1
103
1
0.1
0.01
0.001
0.0001
10-3
106
W
K
10
800
400
200
100
η>30%
η=7%
η=15%
Energy harvesting
Stove/Fireplace
Waste heat from engine
(Car, Co-generation)
Incinerator
Biomass
Industry
Solar heat
Geotherm.
Thermal plant
（Low tem. wast）
η=20%
Thermoelectric
car
Micro-grid
co-generation
Thermoelectric
Power plant
Electrics
Electronics
Energy harvesting
FC.
Geotherm.
Co-gene
Car
Solar heat
Small gene.
Furnace
Ship
Industry
LNG
Biomass
Therm. plant
Air plane
LNG
Geotherm.
Hot spa
FC
Electrics
Electronics
Energy
harvesting
Energy
harvesting
Small generator
Car
Solar heat
Factory Biomass
Ship Therm. plant
Furnace
Co-gen.
Airplane
LNG
Ship・Factory
Car
Co-gen.
Hot spa
Raw sludge
Furnace
Incin.
Space
research
prototype
demonstration
application
2011
2030
2040
Power/unit (W)
Power/unit (W)
Power/unit (W)
Temperature (K)
Temperature (K)
Temperature (K)
Watch
Candle radio
Mosquito trap
Charge pan
Cost
$/Wh
DT
Scale
Module efficiency (%)
DT @ Tc = 300K (K)
Year

## Slide 44
www.spp1386thermoelectrics.de/
Berlin, Oct 2010

## Slide 45
Ausblick zur Thermoelektrik in Deutschland
Landungs- , Wärme und Stofftransport an thermoelektrischen Grenzflächen
Ressourcenschonende TE Materialien, z.B. Substitution von Bi2Te3 und Kontakte
Skalierbare Materialsynthese und innovative Ansätze zum Modulaufbau
Material- und Modulentwicklung jenseits von ZT-Optimierung
Systemintegration und Wärmemanagement
Eine Initiative zur Anwendungsorientierten Grundlagenforschung
Festkörperphysik und Festkörperchemie
Materialwissenschaften und Festkörperphysik
Verfahrens- und Fertigungstechnik
Ganzheitlich
Mikrosystemtechnik, Elektrotechnik und Mikroelektronik

## Slide 46
Material- und Modulentwicklung jenseits von ZT-Optimierung

## Slide 47
Academic Roadmap for Efficient Thermoelectric Materials
Thin Films and Superlattices, Present Materials Systems
Advanced Manipulation at Atomic and Molecular Levels, Extend from Thin Films and Superlattices to Bulk Materials
Creation of High Efficient Materials of Low Impact on Environment, Rich Resources, Low Cost, High Stability
The 1st
The 2nd
The 3rd
Efficiency of Thermoelectric Materials
２０２０
２０３０
２０４０
Nano Structure and Texture control
Improvement in Heat and Oxidation Resistance, Thermal Stability, Chemical Stability, Thermal and Mechanical Properties
Self-Assembly
Control of Lattice Defects
Control of Anisotropy
Spin Seebeck Effect
Nano Interface Control
Synergy Effect
PGEC
Energy Filtering Effect
Rattling Effect
Self-Assenbly Bulk Materials
Nanostructure Built in Materials
Phonon Scattering and Blocking Effects
Materials Design
by Computation Science
Technology of Nanostructure
Manipulation and Synthesis
New Principles and Concepts
Nano Space Engineering
Fusion of Molecular Technologies
Strongly Correlated Electrons
Control of Carriers
Complex
Quantum Mechanical Effects
Molecular Design
Skutterudites
Clathrates
Heusler Alloys
Organic and Inorganic Hybrids
Bi2Te3Alternative Materials
Resonance Level Effects
Electronic Structure and States
Engineering
Chalcopyrites and
Zinc blende Compounds
Control of Network Structures
PbTe System
New Findings from Transport Mechanism of Organic Materials
New Findings of Condensed
System Physics
（From Fermion to Boson）
Realization of Thermal Diode
Explanation of Non-Steady State Behaviors and their Application
Artificial Crystals by Advanced Design of
Electronic Properties and Synthesis Technologies
Crystals without Thermal Conduction
by Confinement of Phonons
Nanowire Superlattices
Silicides
Oxides
Cluster Solids
Organic Systems
Bi2Te3 System
1st Generation
Thin Films and Superlattices: ZT=2〜3
Bulk Materials: ZT=1〜2
2nd Generation
Thin Films and Superlattices: ZT=3〜5
Bulk Materials: ZT=2〜3
Molecular Sheets and Wires
3rd Generation
Thin Films and Superlattices: ZT ≥ 5
Bulk Materials: ZT ≥ 3
Notes: 47