## Slide 1
Effects of Aluminum trifluoride AlF3 impurities on NMC811 /Graphite Lithium-ion battery performance
Slaheddine Jabri, Simon Grundmeier, Markus Etzkorn, Daniel Schröder, Uta Schlickum
Institute of Applied Physics, TU Braunschweig, 38106 Braunschweig, Germany
Institute of Energy and Process Systems Engineering of TU Braunschweig, 38106 Braunschweig, Germany
KFM 24: Focus Session: Battery Materials – Ion Transport, Impurity Effects and Modelling
21. Mars 2024, 12:55–13:15
1

## Slide 2: Introduction
Recycling with low impurities
Working at high voltage
J. Phys. Chem. Lett. 2015, 6, 4653−4672
Al3++ 3 PF6 → 3PF5 + AlF3
Al2O3 + 6 HF → 2 AlF3 + 3 H2O
Al3++3F- → AlF3
AlF3
CoF2
NiF2
2
Impurity
J Electrochem Soc, 164 (7) A1474-A1479 (2017)
Oxidation reaction of electrolyte
Conductivity ionic
Exfoliation
Low performance
Long lifetime
High performance

## Slide 3: Motivation
Al3++ 3 PF6 → 3 PF5 + AlF3
Al2O3 + 6 HF → 2 AlF3 + 3 H2O
Al3++3F- → AlF3
AlF3 impurity effect
on battery performance
AlF3 ??
Structure modification
Electrolyte degradation
LiPF6 +EC+EMC+VC
3
(XPS, Raman Spectroscopy)
(SEM-FIB)
NMC811 active material

## Slide 4: Sample preparation
Sample sets
Battery cell preparation
Cycle numbers | Charge rate | Discharge rate
250 | 1C | 1C
By Simon
PAT-cell
< 1.5 ppm
≈ 0
Argon + Stickstoff
Glove box
Battery cell disassembly
4
Uncontaminated Cell | Contaminated Cell
Electrode NMC811/G vs. Li/Li+ PAT-cells | Electrode NMC811/G vs. Li/Li+ PAT-cells
Glass fiber separator 260 µm | Glass fiber separator 260 µm
Electrolyte 1 m LiPF6 in EC:EMC (3:7) + 2% VC | Electrolyte 1 m LiPF6 in EC:EMC (3:7) + 2% VC
----- | AlF3 impurity (1000 µg/L)
Room temperature
50 °C

## Slide 5: Electrochemical Results
At Room Temperatur
At 50 °C
Discharge capacity decreases in presence of AlF3 impurity
Low battery performance at high temperature
5
%
%
Average
Average

## Slide 6: SEM-FIB results of fresh NMC 811 cathode
1 µm
Primary particle
Carbon Black
5 µm
Secondary particles
6
PVDF

## Slide 7: SEM-FIB results of aged NMC 811 cathode
3 µm
3 µm
Surface of aged cathode NMC811 electrode
Without AlF3
With AlF3
25 °C
50 °C
Thicker CEI layer cover the active material due to degradation of electrolyte
7
Without AlF3
With AlF3
1 µm
Primary particle
1 µm
1 µm
Film
1 µm
3 µm
3 µm

## Slide 8: SEM-FIB results of aged NMC 811 cathode
Cross-section of cathode NMC811
Without AlF3
With AlF3
50 °C
25 °C
Crakes
No significant morphology modification inside the secondary particle
8

## Slide 9: XPS of aged NMC 811 Cathode electrode
PVDF, carbon black
O(C=O)R
PEG (-CH2-CH2-O-)n
9
NMCO lattice , O-C=O
O(C=O)R
PEG (-CH2-CH2-O-)n
P-O salt
Lix PFy+1 Oz
PVDF
LiF
CnFn
LixPFY+1 OZ
3 µm
3 µm

## Slide 10: XPS of aged NMC 811 Cathode electrode
CoF2
10
MnF2
LixPFY+1 OZ
LiF
1 µm
More Metal dissolution from the active material and forms MF2
CoF2
MnF2,
NiF2
LiF
LixPFY+1 OZ

## Slide 11: Polymerisation of Electrolyte
Appearance of Polymer species
Electrolyte degradation due to presence of lewis acid catalysist as Al (OR)3
11
Fresh NMC 811 particle
Aged NMC 811 particle

## Slide 12: Conclusion and Outlook
Discharge capacity decreases in presence of AlF3 impurities
More electrolyte degradation on cathode and anode surface
Increasing of CEI and SEI layer thickness
Polymer species
LixPFY+1 OZ Salt degradation
Formation of metal fluoride CoF2, MnF2, NiF2
Identifying the low AlF3 impurities that could not drastically damage the cell performance
12
1 µm
1 µm
1 µm
Film
1 µm